## Slide 1: A 0.7 V-to-1.0 V 10.1 dBm-to-13.2 dBm 60-GHz Power Amplifier Using Digitally-Assisted LDO Considering HCI Issues
Rui Wu, Yuuki Tsukui, Ryo Minami, Kenichi Okada, and Akira Matsuzawa
Tokyo Institute of Technology, Japan
Notes: 2007/10/29
0
Total 25min
20-22 minutes for talk

## Slide 2: Outline
Background
– 60-GHz field is attractive
Hot-Carrier-Induced Issues
– HCI influence on circuit reliability
Variable-Supply-Voltage PA using Digitally-assisted LDO
– Circuit design & Measurement results
Conclusions
Notes: 2007/10/29
1

## Slide 3: Background
[1] http://www.tele.soumu.go.jp
9-GHz unlicensed bandwidth
Several Gbps wireless communication
e.g. IEEE 802.15.3c
QPSK3.5 Gbps/ch
16QAM7 Gbps/ch

## Slide 4: HCI Issues are Emerging at 60 GHz
 High fmax, suitable for 60-GHz amplifier
 Bad HCI performance
60-GHz power amplifier
Standard
 Good HCI performance
 Low fmax, can’t be used for 60-GHz amplifier
2.4-GHz power amplifier
Thick oxide
Standard
Notes: Thick‐oxide transistors can be considered as devices from previous technology nodes: 0.25 and 0.18 μm. Their reliable operating voltages are 2.5 and 1.8 V, respectively
fmax related to MAG

## Slide 5: Hot-Carrier-Induced (HCI) Effects
Degrade Vth, gm, drain current, and lifetime
Notes: Reliability issue is significant for practical 60-GHz products. HCI (hot-carrier-induced) effects are dominant for the reliability of the advanced CMOS process.
When a large voltage is applied at the drain of the MOSFET, a high lateral-electric field will exist in the channel. The carriers passing through the high field will gain considerable energy and are called as “hot” carriers. Some of these hot carriers can overcome the barrier between the Si and SiO2 and get injected into gate oxide causing various types of oxide damage. Others can create electron-hole pairs by impact ionization. These effects will degrade the drain current, threshold voltage and transconductance. Therefore reduce the lifetime of the MOSFETs

## Slide 6: Tr. Lifetime Measurement Setup
• Lifetime is defined as the time when the saturation drain current (IDSat) decreases by 10% from its unstressed value
Notes: The lifetime is defined as the time when the drain current
of the transistor (IDS) decreases by 10% from the unstressed
value.

## Slide 7: Tr. Lifetime Measurement Procedure

## Slide 8: 65 nm NMOSFET DC Stress Lifetime
Chart: 
| 0.4 | 0.9
 | 8.3928 | 40613625761.9462
 | 9000 | 700 | 100
1/VDS (1/V)
100
102
104
106
108
1010
Lifetime t (s)
[2] E. Takeda et al., IEDL 1983
VGS
VDS
VDS
t
V
Stress condition
VGS = 0.8 V
[2]
Notes: Tr. W 2x10; K=1.5e-7;b=44.6;
Stress Vds=2 V LT=700 s=12 mins, Vds=1.2 V LT=2e09 (2 billion)=63 years;
Stress Vgs=0.8 V;
Sample Vds=1.2 V Vgs=0.8 V
The lifetime is defined as the time when the drain current
of the transistor (IDS) decreases by 10% from the unstressed
value.

## Slide 9: 65 nm NMOSFET RF Stress Lifetime
Chart: 
| 100 | 100000
 | 2.3418 | 23.3641
 | 5 | 6.4935 | 7.2403 | 7.9221 | 8.6039 | 9.1558 | 9.6104 | 10.0974 | 10.5195 | 10.8766 | 11.2338 | 11.8506 | 12.1104
∆IDSat (%)
Freq.=100 MHz,
Po=11 dBm
102
103
104
105
Time (s)
[3] L. Negre et al., JSSC 2012
Vgs
Vds
Stress condition
t
0.8 V
1.2 V
Vds
Vgs
Notes: Tr. W=2x40 um; A=0.5053; n=0.333; Lifetime=8000s=2 hours;
Bias Vds=1.2 V Vgs=0.8 V
Freq. =100MHz
Stress Pin=-1.26 dBm Pout=11 dBm; Vswing about 2.2 V
Sim. Vg_pp=1.1 V; Vd_pp=1.9 V

## Slide 10: Conventional Solutions
[5] M. Tanomura et al., ISSCC 2008
[4] A. Siligaris et al., JSSC 2010
[6] J. Chen et al., ISSCC 2011
 Better lifetime
 Degraded output power, efficiency, and linearity
Cascode [4]
Low Vdd [5]
 Better lifetime, output power, and linearity
 Sensitive to process variations
Power combining [6]
Notes: [2]MINATEC, France [3] NEC [4] UCB, Niknejad
Different phase delay for different paths

## Slide 11: Time-Division Duplex (TDD) Operation
In IEEE 802.11ad, short inter-frame space (SIFS) is indicated to be 3ms
• TDD operation can eliminate the stringent requirement of filtering and extend the available bandwidth for transceivers.
Notes: SIFS determine the time requirement of on/off switching.
Fast awaking is required

## Slide 12: The Proposed Power Amplifier
Notes: Coarse Tr. 4x255=1020 um , Fine Tr. 4x48=192 um
On-chip decoupling cap.=86 pF
R1=R2=50 kohm ,C1=2 pF;
Rfb=5 kohm, Cfb=1 pF;

## Slide 13: Transient Operation of the LDO(1/3)
Notes: Wakeup time is less than 0.1us

## Slide 14: Transient Operation of the LDO(1/3)
Notes: Coarse Tr. 4x255=1020 um , Fine Tr. 4x48=192 um
On-chip decoupling cap.=86 pF
R1=R2=50 kohm ,C1=2 pF;
Rfb=5 kohm, Cfb=1 pF;

## Slide 15: Transient Operation of the LDO(2/3)
Notes: Wakeup time is less than 0.1us

## Slide 16: Transient Operation of the LDO(2/3)
Notes: Coarse Tr. 4x255=1020 um , Fine Tr. 4x48=192 um
On-chip decoupling cap.=86 pF
R1=R2=50 kohm ,C1=2 pF;
Rfb=5 kohm, Cfb=1 pF;

## Slide 17: Transient Operation of the LDO(3/3)
Notes: Wakeup time is less than 0.1us

## Slide 18: Transient Operation of the LDO(3/3)
Notes: Coarse Tr. 4x255=1020 um , Fine Tr. 4x48=192 um
On-chip decoupling cap.=86 pF
R1=R2=50 kohm ,C1=2 pF;
Rfb=5 kohm, Cfb=1 pF;

## Slide 19: Differential PA Topology
The cross-coupling capacitor technique is adopted to improve the stability and power gain
Notes: 2x20 um/0.06 um; 2x30 um/0.06 um; 2x40 um/0.06 um;
Power requirement for each transistor is relieved
The HCI effects on the PA are further alleviated owing to the adoption of the differential topology

## Slide 20: Die Micro-photograph
700 mm
800 mm
Notes: PA core 0.132mm2; LDO 0.025mm2; CL 86 pF, 0.051mm2

## Slide 21: Measured Small-Signal S-parameter
Notes: 3-dB bandwidth is about 13 GHz (from 53 GHz to 66 GHz);
Peak gain =19.7 dB@59 GHz, VPA=1.0 V;
Peak gain =17.0 dB@59 GHz, VPA=0.7 V;

## Slide 22: PA Performance vs VPA @60 GHz
Chart: 
| 0.70000000000000018 | 0.8 | 0.9 | 1
 | 10.1 | 11.1 | 12 | 13.2
 | 5.8 | 7.3 | 8.5 | 10.2
 | 8.1 | 10 | 11.9 | 15
Psat and P1dB (dBm)
VPA (V)
PAEmax (%)
P1dB
Psat
PAEmax

## Slide 23: Measured Lifetime of the PA
Chart: 
| 1 | 10000000000
 | 0.1512 | 71.3759
 | 0.0532 | 45.9105
 | 0.003 | 2.5889
 | 0.80335 | 0.978 | 1.0828 | 1.5718 | 1.5019
 | 0.48883 | 0.66341 | 0.85545 | 0.87291 | 0.89036
 | 0.019113 | 0.038226 | 0.076453 | 0.095566 | 0.095566
∆IDSat (%)
Time (s)
VPA=1.00 V, Pout=10 dBm
VPA=1.00 V, Pout=5 dBm
VPA=0.75 V, Pout=5 dBm
1
102
104
106
108
1010
Notes: VPA=1.00 V, Pout=10 dBm, lifetime=0.2 year;A1=0.1512,N1=0.2674
VPA=1.00 V, Pout=5 dBm, lifetime=1.8 year;A2=0.0532,N2=0.2936
VPA=0.75 V, Pout=5 dBm, lifetime>30 year;A3=0.003,N3=0.294
Freq. = 60 GHz

## Slide 24: Measured Output Spectrum
Chart: 
 | -30 | -30 | -25 | -20 | 0 | 0 | 0 | -20 | -25 | -30 | -30
Centered Freq. (GHz)
Magnitude (dB)
Chart: 
 | -30 | -30 | -25 | -20 | 0 | 0 | 0 | -20 | -25 | -30 | -30
Magnitude (dB)
Centered Freq. (GHz)
(a)
IEEE 802.15.3c Spectrum mask
(b)
Spectrum centered at 62.64 GHz for QPSK modulation
(a) VPA=1.0 V, Pout=4 dBm; (b) VPA=0.7 V, Pout=3 dBm
Notes: channel 3 (61.56 GHz to 63.72 GHz ); symbol rate 1.76 Gs/s

## Slide 25: Measured EVM for QPSK Modualtion
Chart: 
| 0.70000000000000018 | 0.8 | 0.9 | 1
Pout = 5 dBm | -17.7882 | -18.0618 | -18.3443 | -18.6363
Pout = 7 dBm | -17.7882 | -18.1316 | -18.4164
Pout = 10 dBm | -17.3292 | -17.6546
VPA (V)
EVM (dB)
Notes: channel 3 (61.56 GHz to 63.72 GHz ); symbol rate 1.76 Gs/s

## Slide 26: 60 GHz CMOS PA Performance Comparison
† Only for the last stage VPA
[5] M. Tanomura et. al, ISSCC 2008
[6] J. Chen et. al, ISSCC 2011
[4] A. Siligaris et. al, JSSC 2010
Ref. | Process | Vdd (V) | P1dB (dBm) | Psat (dBm) | PAEmax (%) | Lifetime (year)
[4] | 65 nm SOI | 1.2 | 7.1 | 10.5 | 22.3 | N/A
 |  | 1.8 | 12.7 | 14.5 | 25.7 | 
 |  | 2.6 | 15.2 | 16.5 | 18.2 | 
[5] | 90 nm | 0.7 | 5.2 | 8.5 | 7.0 | > 105*
 |  | 1.0 | 10.5 | 11.5 | 8.5 | > 10*
[6] | 65 nm | 1.0 | 15.0 | 18.6 | 15.1 | N/A
[7] | 65 nm | 1.0 | 8.0 | 11.5 | 15.2 | > 10*
This work | 65 nm | 0.7† | 5.8 | 10.1 | 8.1 | > 102
 |  | 1.0† | 10.2 | 13.2 | 15.0 | > 0.2
[7] W. L. Chan et. al, JSSC 2010
* Non-measured results

## Slide 27: Conclusions
– The lifetime of the proposed PA can be improved dramatically by dynamic operation.
– The tunable supply offers a possibility to meet different linearity, efficiency, output power and lifetime requirements in actual applications.
– The PA is insensitive to the process variations thanks to the tunable supply voltage.
Notes: fabricated in a standard 65-nm CMOS process

## Slide 28
Thank you for your attention!